## Slide 1: Sr2RuO4 model information

## Slide 2: Models - Sr2RuO4_Xdeg.dat
Crystal structure is a monolayer of Sr2RuO4 with vacuum in a two Ru atom unit cell configuration.
Oxygen atoms rotated by X degrees centered around Ru atoms, clockwise for Ru atom 1, anticlockwise from Ru atom 2.
Ru-Ru distance were kept constant.
0 degrees
10 degrees

## Slide 3: DFT info
Structural parameters taken from experimental .cif file.
- Vogt and Buttrey, PRB, 52,9843-9846 (1995)
Performed in Quantum Espresso, downfolded using Wannier90
PBE exchange correlation
k = 8x8x1, Ecutrho = 720 Ry, Ecutwfc = 90 Ry

## Slide 4: Electronic structure information
6 band model of the Ru dxz, dyz and dxy states for two Ru atoms.
The Wannier90 file has the orbitals labelled {dxz(Ru1),dyz(Ru1),dxy(Ru1),dxz(Ru2),dyz(Ru2),dxy(Ru2)}
Models with SOC have 12 states, the first 6 are in the same orbital order for the spin up states, the second 6 are equivalent for the spin down states. The SOC strength is 175 meV.
Band structures are coloured according to maximum orbital content

## Slide 5: Sr2RuO4_0deg.dat

## Slide 6: Sr2RuO4_1deg.dat

## Slide 7: Sr2RuO4_2deg.dat

## Slide 8: Sr2RuO4_3deg.dat

## Slide 9: Sr2RuO4_4deg.dat

## Slide 10: Sr2RuO4_5deg.dat

## Slide 11: Sr2RuO4_6deg.dat

## Slide 12: Sr2RuO4_7deg.dat

## Slide 13: Sr2RuO4_8deg.dat

## Slide 14: Sr2RuO4_9deg.dat

## Slide 15: Sr2RuO4_10deg.dat

## Slide 16: Sr2RuO4_11deg.dat

## Slide 17: Sr2RuO4_12deg.dat

## Slide 18: Sr2RuO4_0deg_SOC.dat

## Slide 19: Sr2RuO4_1deg_SOC.dat

## Slide 20: Sr2RuO4_2deg_SOC.dat

## Slide 21: Sr2RuO4_3deg_SOC.dat

## Slide 22: Sr2RuO4_4deg_SOC.dat

## Slide 23: Sr2RuO4_5deg_SOC.dat

## Slide 24: Sr2RuO4_6deg_SOC.dat

## Slide 25: Sr2RuO4_7deg_SOC.dat

## Slide 26: Sr2RuO4_8deg_SOC.dat

## Slide 27: Sr2RuO4_9deg_SOC.dat

## Slide 28: Sr2RuO4_10deg_SOC.dat

## Slide 29: Sr2RuO4_11deg_SOC.dat

## Slide 30: Sr2RuO4_12deg_SOC.dat

## Slide 31: Sr2RuO4_12deg_SOC.dat